## Slide 1: OSR Training #4 Crystalline HPMs

## Slide 2: Why are Plastics used as alternatives to Metals?
Extend Part Life
Reduce/Eliminate Lubrication
Extend Life of Mating Parts
Reduce Weight
Solve Corrosion Issues
Provide Electrical Insulation/ESD
Provide Thermal Insulation

## Slide 3: Thermoplastic Materials

## Slide 4: Quiz Time!

## Slide 5: Polytetrafluoroethylene
(Teflon to you, me, and DuPont)

## Slide 6: PTFE
ADVANTAGES
Low Coefficient of Friction
Chemically Inert
Excellent Electrical Insulator
Low Moisture Absorption
FDA, USDA
LIMITATIONS
Low Strength and Creep Resistance
Poor Thermal Stability
Low Limiting PV
Loose Tolerances
CUT - 500
HDT - 132
Tg - 75

## Slide 7: PTFE Formulations
Virgin High Purity, Toughness
Glass Filled Strength, Stability
Graphite Filled Bearing performance
Carbon Filled Strength,Stability,Wear
MD Filled Wear, Stability
Mica Filled Creep Resistance, Wear
Bronze Filled Strength

## Slide 8: PTFE-Proprietary Grades
Fluorosint 207
  Bearing Grade
Fluorosint 500
  Structural Grade
Fluorosint HPV
  Enhanced Wear
Fluorosint 135
  Higher Strength
Rulon LR (Maroon)
  General Purpose
Rulon J (Gold)
  Non Galling
Rulon 641 (White)
  Bearing Grade
Rulon 123 (Black)
  Higher Strength

## Slide 9: PTFE Application Notes
Temperatures to 500 F
  Can spike to higher
Lightly Loaded
  Low yield strength, modulus
Avoid soft metal mating surface
  Galling may become a problem
Harsh Chemical environments
Best Machining: +/- .001**

## Slide 10: PTFE Applications
Valve Seats
Spools
Pump Wear Rings
Packings
Nozzles
Connectors
Seals
Poppets
Bushings
Washers
Rollers
Insulators
Scrapers
Piston Rings

## Slide 11: Additional Fluoropolymers
FEP Similar Strength, lower temperature
PFA Higher Strength, lower temperature
PVDF Significantly higher Strength and Creep Resistance, lower temperature

## Slide 12: Quiz Time!

## Slide 13: Polyphenylene Sulfide
(PPS—PEEK’s Little Brother)

## Slide 14: PPS (Polyphenylene Sulfide)
ADVANTAGES
High Strength and Stiffness
Excellent Chemical Resistance
Dimensional Stability
Steam Resistance
Low Moisture Absorp.
Ryton or Fortron Resin
LIMITATIONS
Poor Wear Resistance in Unfilled Grades
Limited Abrasion Resistance
Comp. Molded tends to be brittle
CUT - 450
HDT - 230/ 490
Tg - 230

## Slide 15: PPS Formulations
Extruded (Fortron)
Unfilled
Bearing Grade
Compression/Injection Molded (Ryton)
Unfilled
Glass Filled
Bearing Grade
High Purity
Enhanced PV, Wear
Large Shapes
Highest Strength
Enhanced PV, Wear

## Slide 16: PPS Application Notes
Temperatures to 450 F
Clean Environments best
  Poor abrasion resistance
Static applications
  Bearing grade for dynamic situations
Harsh chemical environments
  Stronger than PTFE, less expensive than PEEK
Best Machining +/- .001

## Slide 17: PPS Applications
Pump bodies
Thrust Washers
Valve Components
Bushings
Impellers
Test Fixtures
Manifolds
Lantern Rings
Rotors
Gears
Clamps
Spacers

## Slide 18: Quiz Time!

## Slide 19: Polyetheretherketone
(Versatility—At a Price)

## Slide 20: PEEK (Polyetheretherketone)
ADVANTAGES
Strength and Stiffness
Wear Resistance
Abrasion Resistance
Dimensional Stability
Chemical Resistance
Steam Resistance
Toughness
FDA Compliant
LIMITATIONS
High Coefficient of Friction in Unfilled
Strong Acids (Heavy Concentrations near 1)
CUT - 480
HDT - 320/600
Tg - 290

## Slide 21: PEEK Formulations
Unfilled
30% Glass Reinforced
Bearing Grade
30% Carbon Filled
20% PTFE Filled
Highest Toughness,
Purity
Increased Strength,
Stability
Enhanced PV, Wear
Rates
Highest Strength, PV,
Best Wear
Low Friction, Wear

## Slide 22: PEEK Formulations
Formulation | Flex. Modulus | Limiting PV | K Factor
Unfilled | 600,000 | 8,500 | 375
Bearing Grade | 1,100,000 | 20,000 | 100
Carbon Filled | 1,250,000 | 25,000 | 150
PTFE Filled | 464,000 | 18,000 | 90
Glass Filled | 1,000,000 | -- | --

## Slide 23: PEEK Application Notes
Temperatures to 500 F
  Strength and stability affected over 300 F
Wear Applications
  Filled versions for linear movement
Hostile chemical environments
  Resistance to steam
Best machining +/- .001

## Slide 24: PEEK Applications
Bushings
Seals
Pump Wear Rings
Nozzles
Spools
Rotors
Guides
Back Up Rings
Thrust Washers
Gears
Impellers
Valve Seats
Poppets
Insulators
Rollers
Pistons

## Slide 25: Unlubricated Bushing
110 PSI
117 RPM
1.625” Shaft
219 °F

## Slide 26
Thanks for playing and participating!