## Slide 1: OSR Training #2 Engineering Materials

## Slide 2: Why are Plastics used as alternatives to Metals?
Extend Part Life
Reduce/Eliminate Lubrication
Extend Life of Mating Parts
Reduce Weight
Solve Corrosion Issues
Provide Electrical Insulation/ESD
Provide Thermal Insulation

## Slide 3: Thermoplastic Materials

## Slide 4: HDPE Polypropylene
Chemical Resistance
Toughness
Good Abrasion Resistance
Limited Wear Resistance
CUT 180
HDT 110
Tg 110
Chemical Resistance
Improved Rigidity
Limited Wear / Abrasion Resistance
Better Dimensional Stability
CUT 180
HDT 205
Tg 140

## Slide 5: UHMW (Ultra High Molecular Weight Polyethylene)
ADVANTAGES
Low Coefficient of Friction
Chemically Inert
Abrasion Resistance
Impact Strength
Moderate Wear Resistance
FDA, USDA
LIMITATIONS
Low Strength
Poor Thermal Stability
Low Limiting PV
CUT - 180
HDT - 115
Tg - 115
Machining Difficulties

## Slide 6: UHMW Formulations
Virgin Standard
Reprocessed Economical
UV Resistant Weather Stability
Glass Filled Flow Promotion
Dry Lubricant Lower Friction
Oil Filled Low Friction, FDA
Anti-Static Electrically Conductive
Heat Stabilized Reduced Degradation

## Slide 7: UHMW Application Notes
Temperatures up to 180 F
  Low strength and stability beyond 115 F
Limiting PV of 2,000
  Speeds less than 20 fpm (rotary)
Sliding applications
Dirty, gritty environments
Hostile chemicals
Best machining: +/- .005

## Slide 8: UHMW Applications
Slide Pads
Belt Guides
Star Wheels
Rollers
Sprockets
Valve Seats
Conveyor Flights
Bushings
Wear Strips
Chain Guides
Wheels
Spacers
Insulators
Scrapers

## Slide 10: Nylon (Polyamide)
ADVANTAGES
High Strength and Toughness
Wear Resistance
Abrasion Resistance
Size and Shape Availability
FDA, USDA, 3-A Dairy
LIMITATIONS
Moisture Absorption
Limited Chemical Resistance
CUT - 200/220
HDT - 200
Tg - 145

## Slide 11: Nylon Formulations
Unfilled Natural/Black
Glass Filled Better Strength
Moly Filled Stiffness, Dim. Stability
Impact Modified Toughness
Heat Stabilized Higher Temperature
Oil Filled Lower Wear, Friction
Oil + Moly Low Friction, Stability
Solid Lubricant Better Wear, PV

## Slide 12: Nylon Formulations
Formulation | Comp.Str. | PV Limit | K (Wear)
Type 6/6 | 12,500 | 2,700 | 75
Type 6 | 15,000 | 3,000 | 72
Cast MD | 14,000 | 3,000 | 70
Oil | 12,000 | 5,500 | 68
Oil + MD | 13,000 | 5,600 | 65
NSM | 14,000 | 15,000 | 9
703XL | 10,000 | 17,000 | 18

## Slide 13: Nylon Application Notes
Temperatures up to 220 F
  May change with fillers
Limiting PV to 15,000
  Speeds to 400 fpm
Dry Environments
  Best wear, Dimensional Stability
Wear applications under heavy loads
Best machining: +/- .003

## Slide 14: Nylon Applications
Bushings
Slide Pads
Gears
Sheaves
Guides
Wheels
Cams
Spacers
Bearings
Thrust Washers
Sprockets
Pulleys
Sleeves
Rollers
Cam Followers
Insulators

## Slide 16: Acetal
ADVANTAGES
Strength and Stiffness
Good Dimensional Stability
Wear Resistance when Wet
Machinability
FDA, USDA, 3-A Dairy
LIMITATIONS
Limited Wear Resistance when Dry
Relatively Poor Abrasion Resistance
Limited Chemical Resistance
CUT - 180,HDT - 220
Tg - 150

## Slide 17: Acetal Formulations
COPOLYMER
Reduced Centerline Porosity
Better Chemical Resistance
Better Hot Water Resistance
Less Outgassing
HOMOPOLYMER
Higher Strength
Higher Stiffness
Higher Hardness
Higher HDT
Better CLTE

## Slide 18: Acetal Formulations
Virgin Natural/Black
(Copolymer or Homopolymer)
Glass Filled Higher Strength
PTFE Filled Improved Wear, PV
Anti-Static ESD

## Slide 19: Acetal Application Notes
Temperatures up to 180 F
  Air or Water Temperature
Limiting PV to 8,750
  Speeds to 400 fpm
Wet Environments
  Best wear rates
Tight Tolerances
Best machining: +/- .0015

## Slide 20: Acetal Applications
Bushings
Back Up Rings
Gears
Guides
Spacers
Manifolds
Insulators
Pistons
Slide Pads
Valve Seats
Sprockets
Locators
Thrust Washers
Nozzles
Star Wheels
Rollers

## Slide 22: Polyester (PET-P)
ADVANTAGES
High Strength
Wear Resistance--Wet or Dry
Creep Resistance
Abrasion Resistance
Chemical Resistance
Dimensional Stability
FDA, USDA, 3-A Dairy
LIMITATIONS
Continuous Hot Water
Continuous Steam
Low Impact Properties
CUT - 210
HDT - 240
Tg - 180

## Slide 23: Polyester (PET-P)
ADVANTAGES
High Strength
Wear Resistance--Wet or Dry
Creep Resistance
Abrasion Resistance
Chemical Resistance
Dimensional Stability
FDA, USDA, 3-A Dairy
LIMITATIONS
Continuous Hot Water
Continuous Steam
Low Impact Properties
CUT - 210
HDT - 240
Tg - 180

## Slide 24: Polyester Formulations
Virgin PBT Natural/Black
PBT w/ PTFE Improved wear, PV
Virgin PET Natural/Black
PET w/ PTFE Improved wear, PV

## Slide 25: Polyester Application Notes
Temperatures up to 210 F
  Air only
Limiting PV to 8,000
  Speeds to 400 fpm
Wet or Dry Environments
  Wear rate of Nylon dry, Acetal wet
Abrasive, tight tolerance applications
Best machining: +/- .001

## Slide 26: Polyester Applications
Bushings
Sleeves
Manifolds
Pistons
Cams
Sprockets
Rollers
Slide Pads
Insulators
Guides
Nozzles
Cam Followers
Gears
Wheels

## Slide 27: Material Comparison 1=Best
 | Flexural Modulus | Wear Resistance | Abrasion Resistance | Dim. Stability | Chemical Resistance
UHMW ($0.50) | 4 | 3 | 1 | 4 | 1
Nylon ($1.00) | 2 | 1 | 2 | 3 | 3
Acetal ($1.30) | 3 | 4 | 4 | 2 | 4
PET-P ($1.85) | 1 | 2 | 3 | 1 | 2